## Slide 1
High-throughput experiments elucidate the impact of multicomponent interactions on solute transport in complex feed streams
Laurianne Estrada, Jonathan A. Ouimet, William Phillip

## Slide 2
Single Salt Experiments

## Slide 3
Feed: 1 mM NaCl
Diafiltrate: 150 mM NaCl
Feed: 1 mM CaCl2
Diafiltrate: 75 mM CaCl2
Feed: 1 mM LaCl3
Diafiltrate: 20 mM LaCl3
 | H | H
NaCl |  | 
CaCl2 |  | 
LaCl3 |  | 
NaCl |  | 
CaCl2 |  | 
LaCl3 |  | 

## Slide 4
Multicomponent Experiments

## Slide 5
Nomenclature and Multi Salt Equations
: Main-term solute permeability coefficient for salt 1.
: Main-term solute permeability coefficient for salt 2.
: Cross-term solute permeability coefficient.
Influence of the transport of ion 2 on ion 1.
: Cross-term solute permeability coefficient.
Influence of the transport of ion 1 on ion 2.

## Slide 6
NF270_MC2, 05.08.24_E1
Multicomponent: NaCl, CaCl2
Feed: 10 mM CaCl2
Diafiltrate: 4 mM CaCl2; 50 mM NaCl

## Slide 7
NF270_MC2, 05.08.24_E2
Multicomponent: NaCl, CaCl2
Feed: 20 mM CaCl2
Diafiltrate: 8 mM CaCl2; 50 mM NaCl

## Slide 8
NF270_MC5, 06.05.26_E3
Multicomponent: NaCl, CaCl2
Feed: 10 mM NaCl
Diafiltrate: 5 mM NaCl; 50 mM CaCl2

## Slide 9
NF270_MC5, 06.05.26_E4
Multicomponent: NaCl, CaCl2
Feed: 20 mM NaCl
Diafiltrate: 10 mM NaCl; 50 mM CaCl2

## Slide 10
NF270_MC2, 05.09.24_E5
Multicomponent: NaCl, CaCl2
Feed: 10 mM NaCl; 1 mM CaCl2
Diafiltrate: 50 mM NaCl; 50 mM CaCl2

## Slide 11
NF270_MC2, 05.21.24_E6
Multicomponent: CaCl2, LaCl3
Feed: 5 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM CaCl2

## Slide 12
NF270_MC2, 05.21.24_E7
Multicomponent: CaCl2, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM CaCl2

## Slide 13
NF270_MC2, 05.22.24_E8
Multicomponent: CaCl2, LaCl3
Feed: 10 mM CaCl2
Diafiltrate: 6 mM CaCl2; 15 mM LaCl3

## Slide 14
Multicomponent: CaCl2, LaCl3
Feed: 20 mM CaCl2
Diafiltrate: 12 mM CaCl2; 15 mM LaCl3
NF270_MC5, 09.08.25_E9

## Slide 15
Multicomponent: CaCl2, LaCl3
Feed: 1 mM LaCl3; 5 mM CaCl2
Diafiltrate: 10 mM LaCl3; 25 mM CaCl2
NF270_MC2, 05.22.24_E10

## Slide 16
NF270_MC4, 07.16.24_E17
Multicomponent: CaCl2, LaCl3
Feed: 50 mM CaCl2; 1 mM LaCl3
Diafiltrate: 20 mM LaCl3

## Slide 17
NF270_MC2, 05.28.24_E11
Multicomponent: NaCl, LaCl3
Feed: 10 mM NaCl
Diafiltrate: 5 mM NaCl; 15 mM LaCl3

## Slide 18
NF270_MC2, 05.28.24_E12
Multicomponent: NaCl, LaCl3
Feed: 20 mM NaCl
Diafiltrate: 10 mM NaCl; 15 mM LaCl3

## Slide 19
NF270_MC4, 07.12.24_E13
Multicomponent: NaCl, LaCl3
Feed: 5 mM LaCl3
Diafiltrate: 0.2 mM LaCl3; 50 mM NaCl

## Slide 20
NF270_MC5, 09.09.25_E14
Multicomponent: NaCl, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM NaCl

## Slide 21
NF270_MC2, 05.30.24_E15
Multicomponent: NaCl, LaCl3
Feed: 10 mM NaCl; 1 mM LaCl3
Diafiltrate: 50 mM NaCl; 10 mM LaCl3

## Slide 22
NF270_MC4, 07.16.24_E16
Multicomponent: NaCl, LaCl3
Feed: 50 mM NaCl; 1 mM LaCl3
Diafiltrate: 10 mM NaCl; 20 mM LaCl3