## Slide 1
High-throughput experiments elucidate the impact of multicomponent interactions on solute transport in complex feed streams.
Target Journal: Nature Water
Experimental Results - Analyzed
Laurianne Estrada, Jonathan A. Ouimet, Zhicheng Lu, Molly Dougher, Shammah Lilonfe, Alexander Dowling, William Phillip

## Slide 2
Diafiltration Experiments are Run in a Modified Stirred Cell Apparatus.
Membrane
Retentate Probe
Permeate Probe
Scintillation Vials
Motor
Balance
Pressure Gauge
P
Diafiltrate Tank
Pressure Relief Valve
Stirred Cell
Permeate Outlet
Multiple (two) salts are now placed within the feed and diafiltrate reservoirs.
Retentate and permeate conductivity data are obtained at 5 second intervals.
Scintillation vials are analyzed after the experiment (ICP-OES) to get ion specific concentrations.

## Slide 3
Sodium Chloride Experiments
Single Salt

## Slide 4
Legend
Color depends on the salt
X
Permeability probe conductivity
Retentate probe conductivity
ICP feed and retentate
Bulk permeate conductivity
ICP permeate
Retentate mass balance
ICP feed and retentate
ICP permeate
Stirred cell mass balance

## Slide 5
NF270_MC2, 05.07.24_NaCl
Data Quality: Good
Single Salt: NaCl
Feed: 1 mM
Diafiltrate: 50 mM

## Slide 6
NF270_MC3, 07.09.24_NaCl
Data Quality: Bad
Single Salt: NaCl
Feed: 1 mM NaCl
Diafiltrate: 150 mM NaCl

## Slide 7
NF270_MC3, 07.22.24_SNaCl
Data Quality: Excellent
Single Salt: NaCl
Feed: 150 mM NaCl
Diafiltrate: milliQ water (0 mM NaCl)

## Slide 8
NF270_MC4, 07.11.24_SNaCl
Data Quality: Good
Single Salt: NaCl
Feed: 1 mM NaCl
Diafiltrate: 150 mM NaCl

## Slide 9
NF270_MC5, 07.23.24_NaCl
Data Quality: Excellent
Single Salt: NaCl
Feed: 1 mM NaCl
Diafiltrate: 150 mM NaCl

## Slide 10
NF270_MC5, 07.23.24_SNaCl
Data Quality: Good
Single Salt: NaCl
Feed: 1 mM NaCl
Diafiltrate: 150 mM NaCl

## Slide 11
NF270_MC5, 07.23.24_S2NaCl
Data Quality: Excellent
Single Salt: NaCl
Feed: 100 mM NaCl
Diafiltrate: milliQ (0 mM NaCl)

## Slide 12
NF270_MC5, 05.27.26_NaCl
Data Quality: Excellent
Single Salt: NaCl
Feed: 1 mM
Diafiltrate: 150 mM

## Slide 13
Calcium Chloride Experiments
Single Salt

## Slide 14
NF270_MC2, 05.07.24_CaCl2
Data Quality: Good
Single Salt: CaCl2
Feed: 1 mM
Diafiltrate: 50 mM

## Slide 15
NF270_MC3, 07.11.24_CaCl2
Data Quality: Good
Single Salt: CaCl2
Feed: 1 mM CaCl2
Diafiltrate: 50 mM CaCl2

## Slide 16
NF270_MC3, 07.11.24_SCaCl2
Data Quality: Good
Single Salt: CaCl2
Feed: 1 mM CaCl2
Diafiltrate: 50 mM CaCl2

## Slide 17
NF270_MC3, 07.12.24_S2CaCl2
Data Quality: Bad
Single Salt: CaCl2
Feed: 1 mM CaCl2
Diafiltrate: 50 mM CaCl2

## Slide 18
NF270_MC5, 05.27.26_CaCl2
Data Quality: Good
Single Salt: CaCl2
Feed: 1 mM CaCl2
Diafiltrate: 75 mM CaCl2

## Slide 19
NF270_MC5, 06.27.26_CaCl2
Data Quality: Good
Single Salt: CaCl2
Feed: 1 mM CaCl2
Diafiltrate: 75 mM CaCl2

## Slide 20
Lanthanum Chloride Experiments
Single Salt

## Slide 21
NF270_MC2, 05.21.24_LaCl3
Data Quality: Excellent
Single Salt: LaCl3
Feed: 1 mM
Diafiltrate: 20 mM

## Slide 22
NF270_MC4, 07.11.24_SLaCl3
Data Quality: Good
Single Salt: LaCl3
Feed: 1 mM LaCl3
Diafiltrate: 20 mM LaCl3

## Slide 23
Multicomponent Experiments

## Slide 24
NF270_MC2, 05.08.24_E1
Data Quality: Excellent
Multicomponent: NaCl, CaCl2
Feed: 10 mM CaCl2
Diafiltrate: 4 mM CaCl2; 50 mM NaCl

## Slide 25
NF270_MC2, 05.08.24_E2
Data Quality: Excellent
Multicomponent: NaCl, CaCl2
Feed: 20 mM CaCl2
Diafiltrate: 8 mM CaCl2; 50 mM NaCl

## Slide 26
NF270_MC5, 06.01.25_E3
Data Quality: Good
Multicomponent: NaCl, CaCl2
Feed: 10 mM NaCl
Diafiltrate: 5 mM NaCl; 50 mM CaCl2

## Slide 27
NF270_MC5, 06.05.26_E3
Data Quality: Excellent
Multicomponent: NaCl, CaCl2
Feed: 10 mM NaCl
Diafiltrate: 5 mM NaCl; 50 mM CaCl2

## Slide 28
NF270_MC5, 06.01.26_E4
Data Quality: Good
Multicomponent: NaCl, CaCl2
Feed: 20 mM NaCl
Diafiltrate: 10 mM NaCl; 50 mM CaCl2

## Slide 29
NF270_MC5, 06.05.26_E4
Data Quality: Excellent
Multicomponent: NaCl, CaCl2
Feed: 20 mM NaCl
Diafiltrate: 10 mM NaCl; 50 mM CaCl2

## Slide 30
NF270_MC2, 05.09.24_E5
Data Quality: Good
Multicomponent: NaCl, CaCl2
Feed: 10 mM NaCl; 1 mM CaCl2
Diafiltrate: 50 mM NaCl; 50 mM CaCl2

## Slide 31
NF270_MC2, 05.21.24_E6
Data Quality: Good
Multicomponent: CaCl2, LaCl3
Feed: 5 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM CaCl2

## Slide 32
NF270_MC2, 05.21.24_E7
Data Quality: Good
Multicomponent: CaCl2, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM CaCl2

## Slide 33
NF270_MC2, 05.22.24_E8
Data Quality: Good
Multicomponent: CaCl2, LaCl3
Feed: 10 mM CaCl2
Diafiltrate: 6 mM CaCl2; 15 mM LaCl3

## Slide 34
Data Quality: Excellent, but LaCl3 concentration is essentially zero
Multicomponent: CaCl2, LaCl3
Feed: 20 mM CaCl2
Diafiltrate: 12 mM CaCl2; 15 mM LaCl3
NF270_MC2, 05.22.24_E9
NEEDS TO BE RERUN

## Slide 35
Data Quality: Good
Multicomponent: CaCl2, LaCl3
Feed: 20 mM CaCl2
Diafiltrate: 12 mM CaCl2; 15 mM LaCl3
NF270_MC5, 09.08.25_E9

## Slide 36
Data Quality: Good
Multicomponent: CaCl2, LaCl3
Feed: 1 mM LaCl3; 5 mM CaCl2
Diafiltrate: 10 mM LaCl3; 25 mM CaCl2
NF270_MC2, 05.22.24_E10

## Slide 37
NF270_MC2, 05.28.24_E11
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 10 mM NaCl
Diafiltrate: 5 mM NaCl; 15 mM LaCl3

## Slide 38
NF270_MC2, 05.28.24_E12
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 20 mM NaCl
Diafiltrate: 10 mM NaCl; 15 mM LaCl3

## Slide 39
NF270_MC2, 05.29.24_E13
Data Quality: Good
Multicomponent: NaCl, LaCl3
Feed: 5 mM LaCl3
Diafiltrate: 0.2 mM LaCl3; 50 mM NaCl
RERUN ON MF270_MC4

## Slide 40
NF270_MC4, 07.12.24_E13
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 5 mM LaCl3
Diafiltrate: 0.2 mM LaCl3; 50 mM NaCl

## Slide 41
NF270_MC2, 05.29.24_E14
Data Quality: Okay
Multicomponent: NaCl, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM NaCl
RERUN ON NF270_MC4

## Slide 42
NF270_MC4, 07.15.25_E14
Data Quality: Bad
Multicomponent: NaCl, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM NaCl
NEEDS TO BE RERUN

## Slide 43
NF270_MC5, 09.09.25_E14
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 10 mM LaCl3
Diafiltrate: 0.4 mM LaCl3; 50 mM NaCl

## Slide 44
NF270_MC2, 05.30.24_E15
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 10 mM NaCl; 1 mM LaCl3
Diafiltrate: 50 mM NaCl; 10 mM LaCl3

## Slide 45
NF270_MC5, 07.16.24_E16
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 50 mM NaCl; 1 mM LaCl3
Diafiltrate: 10 mM NaCl; 20 mM LaCl3

## Slide 46
NF270_MC5, 06.01.26_E16
Data Quality: Excellent
Multicomponent: NaCl, LaCl3
Feed: 50 mM NaCl; 1 mM LaCl3
Diafiltrate: 10 mM NaCl; 20 mM LaCl3

## Slide 47
NF270_MC4, 07.16.24_E17
Data Quality: Excellent
Multicomponent: CaCl2, LaCl3
Feed: 50 mM CaCl2; 1 mM LaCl3
Diafiltrate: 20 mM LaCl3