## Slide 1: Plan for a Digital Twin Testbed
Keshav Kasturi Rangan
Group Meeting
April 2, 2026
From Parameter Estimation to Adaptive Experiment Design in Diafiltration Systems
Digital Model (Current Setup)

## Slide 2: Membrane Characterization using a Digital Model
Prior
Knowledge
Model(s)
Uncertainty Acceptable?
Model with Quantified Uncertainty
No
Yes
Sensitivity & Uncertainty Analysis
Parameter Estimation
Model-Based Design of Experiments
Experimental Data
• Dotted lines ⇢ manual data transmission
• Solid lines → automatic data transmission
Notes: “Membrane characterization can be formulated as a dynamic inverse problem, where we estimate transport parameters from time-resolved experimental data.”
“However, these parameters are often poorly identifiable due to strong correlations, which leads to an ill-conditioned inference problem.”
“To address this, we adopt a closed-loop uncertainty quantification framework.”
👉 (point to diagram)
“We estimate parameters using weighted least squares, quantify uncertainty through sensitivities and the Fisher Information Matrix, and then design new experiments to improve identifiability.”
“This creates a sequential learning loop.”
Final line (slow down):
“Our goal is to reshape the information geometry of the problem so that the parameters become identifiable.”

## Slide 3
From Dynamic Inference to Uncertainty-Aware Digital Twins
Next Stage — Digital Shadow
Real-time experimental data, , used for state estimation,
Online parameter estimation + UQ
Final Stage — Self-Driving Lab
MBDoE selects optimal next experiment
Inner loop → set-point tracking
Close the loop: experiment → estimate → UQ → MBDoE → experiment
This transforms parameter estimation and uncertainty quantification into adaptive experimental learning
Figure adapted from Kritzinger et al. (2018), “Digital Twin in Manufacturing: A Categorical Literature Review and Classification,” IFAC‑PapersOnLine.
Current Stage — Digital Model
Physics-based dynamic model, (DAE system)
Parameters, , estimated from diafiltration experiments
Uncertainty quantified via FIM / covariance
Model predicts next best operating condition
Notes: This is no longer a static workflow — it is a feedback system

## Slide 4
Supervisory Control
Time scale: Hours (~1 hr)
Uncertainty quantification
Model selection based on MBDoE
n-degrees of freedom • Start-up mode • Pressure schedule • Termination condition
Regulatory Control
Time scale: Seconds (~5 sec)
Degrees of freedom/Inputs: 2 • Applied pressure, • Feed concentration,
State estimation
Real-time Monitoring
Time scale: Minutes (~5 min)
Parameter estimation
Fault detection
Medium Loop (minutes)
Notes: “Even with the same model, different experiments can produce very different information about the parameters.”
(point to filtration)
“Filtration operates over a relatively narrow concentration range.”
(point to diafiltration)
“In contrast, diafiltration sweeps the system across a much broader range of operating conditions.”
(pause)
“The question is: which experiment actually makes the parameters identifiable?”
Information is not a property of the model — it is a property of the experiment

## Slide 5: Backup Files
📎

## Slide 7
Notes: “Even with the same model, different experiments can produce very different information about the parameters.”
(point to filtration)
“Filtration operates over a relatively narrow concentration range.”
(point to diafiltration)
“In contrast, diafiltration sweeps the system across a much broader range of operating conditions.”
(pause)
“The question is: which experiment actually makes the parameters identifiable?”
Information is not a property of the model — it is a property of the experiment

## Slide 8: Separation using a Dynamic Diafiltration Device
Membrane
Retentate Probe
Permeate Probe
Scintillation Vials
Motor
Balance
Pressure Gauge
P
Diafiltrate Tank
Pressure Relief Valve
Stirred Cell
Permeate Outlet

## Slide 9
Membrane
Retentate Probe
Permeate Probe
Scintillation Vials
Motor
Balance
Pressure Gauge
P
Diafiltrate Tank
Pressure Relief Valve
Stirred Cell
Permeate Outlet

## Slide 10: Dynamic Model w/ Lumped Parameter Infers Membrane Properties
Concentration
polarization
Parameter Estimation:

## Slide 11: Lumped Parameter Model Infers Membrane Properties
Concentration polarization
[Fig.] Ouimet, J. A. et. al., (2022). Journal of Membrane Science, 641, 119743.
Forward Model
where,
Notes: model parameters, hydraulic permeability Lp, solute permeability coefficient B that correspond to the membrane transport properties,
and reflection coefficient sigma that depends on the thermodynamics of the membrane-solution interface.

## Slide 12: DATA: Diafiltration Apparatus for high-Throughput Analysis
[Fig.] Ouimet, J. A. et. al., (2022). Journal of Membrane Science.
William Phillip
Jonathan Ouimet
Alexander Dowling
Xinhong Liu
How model-based data analytics help improve membrane characterization?

## Slide 13: Dynamic Diafiltration Experiment Sweeps Larger Concentration Space
1
Diafiltrate Reservoir
Experimental degrees of freedom: temperature, pressure, feed concentration, diafiltration concentration

## Slide 14: Dynamic Diafiltration Experiment Sweeps Larger Concentration Space 5x Faster Than Filtration Experiments
Diafiltrate Reservoir

## Slide 15: Fast Reaction is Preferred in Membrane Functionalization
Janus membranes
[Top, Mid. Fig.] Hoffman, J. R., & Phillip, W. A. (2020). ACS Macro Letters, 9(9), 1267-1279.
Fast reaction creates clear boundary and enables precise chemical patterning.
Reactive inks

## Slide 16
Confidence ellipse for covariance matrix
FIM Highlights Nonidentifiable Parameters
Estimated parameters |  | Residuals squared | Eigenvalues of FIM | Eigenvectors of FIM | 
8.16 | 6.18 | 10.74 | -7.02×10-8 | 3.32×10-8 | -1.00
 |  |  | 2.10×102 | -1.00 | -3.32×10-8
Estimated parameters |  | Residuals squared | Eigenvalues of FIM | Eigenvectors of FIM | 
8.16 | 6.18 | 10.74 | -7.02×10-8 | 3.32×10-8 | -1.00
 |  |  | 2.10×102 | -1.00 | -3.32×10-8
Fisher information matrix (FIM)
FIM inference
Model predictions are insensitive to
FIM is rank deficient with Near zero eigenvalue pointing
Solely pH cannot identity in Step 1 model