## Slide 1
Diafiltration to Capture Multicomponent Effects
Jonathan Aubuchon Ouimet, Laurianne Lair, Xinhong Liu, Alexander Dowling, William Phillip

## Slide 2
Diafiltration Capabilities Will Provide an Edge on Understanding Fundamental Phenomena that Govern Multicomponent Transport
Lair et al. Annual Reviews
3000 µS cm-1
Membrane
Retentate Probe
Conductivity Boards
Permeate Outlet
Stir Bar
450.0 µS cm-1
Permeate Probe
Systematic studies on multicomponent interactions are lacking.
Now, diafiltration enables ‘continuous’ monitoring of retentate and permeate measurements.

## Slide 3
Overarching Questions
What ionic strength/ion ratios do multicomponent interactions begin to occur?
How does membrane nanostructure (i.e., charge density) effect multicomponent interactions?
How can
Lair et al. Annual Reviews

## Slide 4
Concentrating
Diafiltrate: 5 mM KCl
Ouimet, et al., J. Membr. Sci., 2022
Kilmartin et. al., I&EC, 2021.
Diafiltration can Operate in Three Distinct Regimes
Critical
Diafiltrate: 1.5 mM KCl
Diafiltrate: 1.8 mM KCl
Diluting
Diafiltrate: 0 mM KCl
NF90 Membranes, Solute: KCl
Notes: Change plot to be the amount of solution that permeated.
Concentrating Regime – Diafiltrate: 5 mM KCl
Critical Regime – Diafiltrate: 1.5 mM KCl (black), 1.8 mM KCl (red)
Diluting Regime – Diafiltrate: 0 mM KCl

## Slide 5
Single Component KCl Experiments

## Slide 6
Single Component NdCl3 Experiments

## Slide 7
Multicomponent KCl, NdCl3 Experiments
Feed: 10 mM KCl, 0 mM NdCl3
Diafiltrate: 5.5 mM KCl, 30 mM NdCl3

## Slide 8
KCl Rejection is More Strongly Dependent on Ionic Strength than KCl:NdCl3 Ratio

## Slide 9
Likely not the first figure, but displaying information in this way creates a figure that is ‘extremely’ information dense.
* Figure will likely hold continuous diafiltration data from ~6 unique experiments, providing ~ 104 data points.
Can we ‘break’ down this data to validate/generate equations on
The molecular scale to enable reverse engineering of membrane materials (rejection as a function of transport coefficients)?
The systems scale to inform modular membrane design. (Rejection as a function of species/salt concentration)

## Slide 10
Similair to previous graph yet aims to be ‘easier’ to understand.
The 3D graph is broken up into slices that are ‘exploded’ in the upper panels. Currently, most data is shown as 2D plots, yet we hypothesize that this removes a significant amount of important information that explains when multicomponent interactions are important.

## Slide 11
Synthesize 3 copolymer membranes with different charge densities.
Show… Pore size is constant, charge density is tunable. Characterize copolymers using suggested experiments.
While an experimentalist engineered 6 unique experiments to characterize membranes (how much information is generated), theory/modeling can propose # experiments to generate # more information.
Notes: Can this be explored by changing the salt identities instead of the