## Slide 1: Investigating the Impact of Multicomponent Interactions on Solute Transport via High-Throughput Experiments
Laurianne Estrada, Jonathan A. Ouimet, Keshav K. Rangan, Shammah Lilonfe, Molly Dougher, Zhicheng Lu, Alexander Dowling, William Phillip
2.11.26

## Slide 2: Figure S1 – Membrane Transport Schematic

## Slide 3: Transport and Thermodynamic Equations
Boundary Layer
Membrane: is found in each term
Bulk
two cations, one anion

## Slide 4: Back-of-the-Envelope Calculations
Knowns | Reasonable Estimates | Unknowns
 | – membrane charge density | 
 | – boundary layer | 
 | – boundary layer | 
 | – boundary layer | 
l – membrane thickness |  | 
Knowns | Reasonable Estimates | Unknowns
l – membrane thickness |  | 
Calculate the reasonable estimates parameters.
Calculate the unknowns.

## Slide 5: Back-of-the-Envelope Calculations
Experiment: NF270_MC2_05.08.24_E1
For vial 1:
Knowns | 
(mM) | 7.07
(mM) | 10.30
(mM) | 27.67
(mM) | 2.56
(mM) | 4.11
(mM) | 10.78
(m2/s) | 1.33e-9
(m2/s) | 0.79e-9
(m2/s) | 2.03e-9
(m3/m2*s) | 9.11e-6
 | 1
 | 2
 | -1
Knowns | 
 | 7.07
 | 10.30
 | 27.67
 | 2.56
 | 4.11
 | 10.78
 | 1.33e-9
 | 0.79e-9
 | 2.03e-9
 | 9.11e-6
 | 1
 | 2
 | -1
Salts: NaCl, CaCl2
Obtain known parameters from experimental data
Reasonable Estimates | 
(mM) | -44
l – membrane thickness (m) | 100e-9
 | 0.21
Reasonable Estimates | 
 | -44
l – membrane thickness (m) | 100e-9
 | 0.21
1. Calculate the reasonable estimate parameters from the literature.
Notes: NF270 DATA2: concentration of KCl in chi calculation was set to 10mM but was supposed to be 1mM. That is why the paper says -140mM but here it says -44mM.

## Slide 6: Back-of-the-Envelope Calculations
Experiment: NF270_MC2_05.08.24_E1
Salts: NaCl, CaCl2
1b. Boundary Layer,
: average velocity, stir bar rate*radius = 350*pi*0.0254/2/60 m/s
: kinematic viscosity = 1.003E-6 m2/s
: stirred cell diameter = 0.0254 m
1a. Mackie & Meares to estimate
1c. Estimate by solving the following system of equations:
Reasonable Estimates | 
(m2/s) | 1.83e-11
(m2/s) | 1.09e-11
(m2/s) | 2.79e-11
(m) | 8.80e-5
(m) | 7.41e-5
(m) | 1.01e-4
(mM) | 
(mM) | 
(mM) | 
Reasonable Estimates | 
 | 1.83e-11
 | 1.09e-11
 | 2.79e-11
 | 8.80e-5
 | 7.41e-5
 | 1.01e-4
1. Calculate the reasonable estimate parameters.
Notes: Mackie & Meares model: 1) polymer chains are hard obstacles and the ion must diffuse around these through the water volume pockets (tortuosity). 2) no specific interactions. 3) uniform swelling. 4) small, simple ions (Na+, Cl-). 5) polymer chains arranged in a cubic lattice.
Stuck at solving the system of equations for c,int. Will be working through this as next steps, but generally this is the current workflow.

## Slide 7: Next Steps & Upcoming Work
Next order of business:
  Estimate
  Estimate
  Calculate
  Repeat for vials 1-10
2. Calculate the unknown variables.
Unknowns
Unknowns
2a. Estimate by solving the following system of equations:
2b. Calculate the partition coefficient, .
These calculations allow us to solve for and back out a solute permeability coefficient, B, for each salt in each vial.
2c. Calculate the solute permeability coefficient, .

## Slide 8: Full equations
Boundary Layer
Bulk

## Slide 9: Full equations
Membrane