Section 4: Analysis

All following calculations were performed in MATALB R2023b. The analysis is performed for each experimental vial collected (10 vials/experiment).

Define variables:

| Knowns | Reasonable Estimates | Unknowns |
| --- | --- | --- |
| c1s,r | χ | c1s,int |
| c2s,r | ϕw | c2s,int |
| c3s,r | l | c3s,int |
| c1s,p | δ1 | c1m,r |
| c2s,p | δ2 | c2m,r |
| c3s,p | δ3 | c3m,r |
| D1s | D1m | H1 |
| D2s | D2m | H2 |
| D3s | D3m | H3 |
| Jw |  |  |
| z1 |  |  |
| z2 |  |  |
| z3 |  |  |

- Read and input the known parameters, in which the retentate concentration (cis,r), permeate concentration (cis,p), and water flux (Jw) are obtained from experimental data.

  - As a representative example, experiment NF270_MC2_05.08.24_E1, vial 1, is selected to outline the back of the envelope calculations.

| Knowns |  |
| --- | --- |
| cNas,r (mM) | 7.07 |
| cCas,r (mM) | 10.30 |
| cCls,r (mM) | 27.67 |
| cNas,p (mM) | 2.56 |
| cCas,p (mM) | 4.11 |
| cCls,p (mM) | 10.79 |
| DNas (m2/s) | 1.33e-9 |
| DCas (m2/s) | 0.79e-9 |
| DCls (m2/s) | 2.03e-9 |
| Jw (m3/m2s) | 9.11e-6 |
| zNa | 1 |
| zCa | 2 |
| zCl | -1 |

- Calculate the reasonable estimate parameters.

  - χ is obtained from zeta potential measurements.

  - The water volume fraction, ϕw, is obtained from the literature.

  - Membrane thickness, l, is obtained from the literature.

  - The boundary layer, δ, is estimated from single salt experiments using the thin-film model. An average value is taken, considering each ion present in the feed solution.

δi=Diki

ki=0.23v00.57Dis0.67ν0.24b0.43= m/s

  - Estimate the membrane diffusion coefficient, Dim, using the Mackie & Meares model.

DimDis=ϕw2-ϕw2

| Reasonable Estimates |  |
| --- | --- |
| χ (mM) | -44 |
| ϕw | 0.21 |
| l (nm) | 100 |
| δNa (m) | 5.93E-5 |
| δCa (m) | 4.99E-5 |
| δCl (m) | 6.81E-5 |
| δavg (m) | 5.91E-5 |
| DNam | 1.83E-11 |
| DCam | 1.09E-11 |
| DClm |  |

- Calculate the unknown variables.

  - Estimate the interfacial concentration of each ion, cis,int. Recall equations 25 and 26,

| Jwcp,1s=c1sJw+∇c1sD11s+∇c2sD12s | Eq 25 |
| --- | --- |

| Jwcp,2s=c2sJw+∇c1sD21s+∇c2sD22s | Eq 26 |
| --- | --- |

In compliance with the nomenclature, Na+ is represented as “1”, Ca2+ is represented as “2”, and Cl- as “3”.

The multicomponent flux equations parallel those for single salt solutions. In this manner, we aim to describe multi-component diffusion in a mathematically simple way. First, we take the partial differential equation for a binary solution

∂c∂t=Dij∂2c∂z2

Here, the diffusion coefficient, Dij, is assumed to be independent of concentration. Additionally, the volume-average velocity of the solvent, in our case water, is assumed to be zero. This eliminates the convection term within the continuity equation.

We can write a transformed concentration, c=tψ, where

t∂ψ∂t=Dijt∂2ψ∂z2

Here, Dij can be written as,

Dij=D11D12D21D22=tσijt-1

where t is the modal matrix whose columns are the eigenvectors of the diffusion coefficient and σi is a diagonal matrix of the eigenvalues of the diffusion coefficient.

t11t12t21t22=1D12D22-σ1D22-σ2D121=1D11-σ1D21D21D11-σ21

σ1=12D11+D22+(D11-D22)2+4D12D21

σ2=12D11+D22-(D11-D22)2+4D12D21

Multiplying the partial differential equation by the inverse of the modal matrix allows us to convert the transformed concentrations back into measured concentrations.

t-1t∂ψ∂t=t-1Dijt∂2ψ∂z2

We can further simplify to

∂ψ∂t=σij∂2ψ∂z2

which is synonymous with the partial differential equation for concentration above. Key differences to note here are that we are using a transformed concentration, ψi, and rather than a binary diffusion coefficient we have the eigenvalue σij.

Since we know the solution for a binary solution concentration gradient is

Δci=FD,z,tΔci0

Then,

Δψ=Fσ,z,tΔψ

And

Δc=tFσ,z,tt-1Δc0

Since we are interested in calculating the interfacial concentrations of each ion in a multicomponent system, we can take the binary solution and apply it to our ternary system. For a binary system,

cis,int-cis,pcis,r-cis,p=exp⁡(JwδD)

Therefore,

ψis,int-ψis,pψis,r-ψis,p=exp⁡(Jwδσ)

If we define

Δψa=ψint-ψs,p; Δca=cint-cs,p

Δψ0=ψs,r-ψs,p; Δc0=cs,r-cs,p

Δca=texp⁡(Jwδσ)t-1Δc0

Taking the definition for the eigenvalues and eigenvectors above, we obtain the equations

Δc1a=D11-σ2Δc10+D12Δc20σ1-σ2expJwδσ1+D11-σ1Δc10+D12Δc20σ2-σ1expJwδσ2

Δc2a=D22-σ2Δc20+D21Δc10σ1-σ2 exp⁡(Jwδσ1)+D22-σ1Δc20+D21Δc10σ2-σ1expJwδσ2

With these equations, we can solve for the interfacial concentrations by

c1int=Δc1a+c1s,p

c2int=Δc2a+c2s,p

To ensure that the assumptions uphold to the simplification on the multicomponent system equations, we regress the interfacial concentrations using a regression of the ODE without transforming of variables. This serves as a check of the assumptions made above. In this manner, the solute flux equations are organized into the following matrices:

| Jwcp,1s-Jwc1sJwcp,2s-Jwc2s=∇c1s∇c2s D11sD12sD21sD22s | Eq 67 |
| --- | --- |

Solving the simplified equations above, and using the ode15 solver, we compare the interfacial concentrations:

| Unknown Variables – vial 1 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Variable | ODE15 | Simplification | Percent Difference (%) |
| c1s,int | 9.77 | 9.64 | 1.34 |
| c2s,int | 4.51 | 4.58 | 1.54 |

Here, we see strong agreement between the interfacial concentration values calculated using an ODE solver and the simplification. This indicates that the assumptions made above, where we collapse the multicomponent flux equation to that of a binary system by using a transformed concentration, upholds.

  - Estimate the lumped solute permeability coefficient, B.

Starting with Fick’s second law,

0=∂2ci∂z2

with boundary conditions

ciz=0=Hici0

ciz=l=Hicip

Solving for the concentration profiles yields

ciz=Hici0-zlHi(ci0-cip)

Solving for the solute flux gives,

ji=DiHilci0-cip=Biici0-cip

Here, the term DiHil is generally defined as a lumped parameter, Bi, also known as the binary solute permeability coefficient. For our system, we use single salt experiments to estimate Bii for each salt, NaCl, CaCl2, and LaCl3.

We use matrix math in these derivations to standardize the form in which variables are represented. In this way, increasing the number of ions in solution does not change the structure, only the size, of how each variable is expressed. Additionally, matrices simplify the calculation of variables in MATLAB.
Bij=B11B12B21B22

The  following equations are used to define the main Bii coefficients,

Jwcp,is=Bii(cis,int-cis,p)

B11=Jwc1s,pc1s,int-c1s,p

B22=Jwc2s,pc2s,int-c2s,p

Since we are working within the Fickian diffusion framework, the solute flux can be generalized for n-component mixtures such that,

jis= DiiHilcis,int-cis,p+DijHjlcjs,int-cjs,p=Biicis,int-cis,p+Bijcjs,int-cjs,p

jjs= DjiHilcis,int-cis,p+DjjHjlcjs,int-cjs,p=Bjicis,int-cis,p+Bjjcjs,int-cjs,p

Analogous to eq 67, the diffusion coefficient matrix for a multicomponent system comes from organizing jis and jjs in matrix form.

Dij=D11D12D21D22

Rearranging these equations for the cross-solute permeability coefficients,

Jwcp,is= Biicis,int-cis,p+Bij(cjs,int-cjs,p)

B12=Jwc1s,p-B11(c1s,int-c1s,p)c2s,int-c2s,p

B21=Jwc2s,p-B22(c2s,int-c2s,p)c1s,int-c1s,p

Resulting in a solute permeability matrix that looks like,

Bij=B11B12B21B22

Bij=Jwc1s,pc1s,int-c1s,pJwc1s,p-B11(c1s,int-c1s,p)c2s,int-c2s,pJwc2s,p-B22(c2s,int-c2s,p)c1s,int-c1s,pJwc2s,pc2s,int-c2s,p

Non-zero cross solute permeability coefficients represent a deviation from ideality, or solute-solute interactions, where the presence of a competing ion hinders or promotes the diffusion of the other ion present. In a multisalt experiments, performance is different than a single salt experiment.

  - Estimate the partition coefficients, Hi.

First, we assume that there is no accumulation such that the solute flux through the boundary layer is equal to the solute flux through the membrane. For the multicomponent system, we show

| Jwc1p=∇c1mD11m+∇c2mD12m | Modified Eq 45 |
| --- | --- |
| Jwc2p=∇c1mD21m+∇c2mD22m | Modified Eq 46 |

For comparison, we can derive a Hitheo rooted in Donnan exclusion principles. Here, the goal is to define a relationship for c1m that enables us to solve for its value. First, recall equation 50,

μim,0+RTlncim+ziFϕm=μis,0+RTlncis+ziFϕs

We define,

δi0=μi0,s-μi0,mRT

We solve the above equation such that,

ϕm-ϕs=RTziFμi0,s-μi0,mRT+lnciscim

For a 1:1 salt, such as NaCl, where Na is the cation “1” and Cl is the anion “3”. The membrane is assumed to be negatively charged such that -|χ|, thereby making the anion “3” the co-ion. Let us now solve for the co-ion concentration in the membrane.

RTz1Fμ10,s-μ10,mRT+lnc1sc1m=RTz3Fμ30,s-μ30,mRT+lnc3sc3m

μ10,s-μ10,mRT+lnc1sc1m=-μ30,s-μ30,mRT-lnc3sc3m

μ10,s-μ10,mRT+μ30,s-μ30,mRT=-lnc1sc1m-lnc3sc3m

μ10,s-μ10,mRT+μ30,s-μ30,mRT=lnc1mc1s+lnc3mc3s

expμ10,s-μ10,mRT+μ30,s-μ30,mRT=c1mc1sc3mc3s

δ10δ30=c1mc1sc3mc3s

c1sc3sδ10δ30=c1mc3m

Maintaining electroneutrality such that,

z1c1s+z3c3s=0

z1c1m+z3c3m-|χ|=0

We can plug in the c1s and c1m terms,

c3sc3sδ10δ30=(c3m-|χ|)c3m

c3s2δ10δ30=c3m2-|χ|c3m

We set δ10δ30=δ* and obtain the co-ion form.

c3m2-χc3m-c3s2δ*=0

Taking this one step further where we define Hi=cimcis, divide each term by c3s2,

H32-χc3sH3- δ*=0

The steps outlined above can be repeated to solve for the counter-ion “1” as well.

We can repeat the above steps for a 2:1 (CaCl2) and 3:1 (LaCl3) salt, where we want to solve for the co-ion “3”.Here, the steps remain the same however z1 changes to +2 and +3, respectively. The steps to solve for a 2:1 salt are shown below,

RTz1Fμ10,s-μ10,mRT+lnc1sc1m=RTz3Fμ30,s-μ30,mRT+lnc3sc3m

μ10,s-μ10,mRT+lnc1sc1m=-2μ30,s-μ30,mRT+lnc3sc3m

μ10,s-μ10,mRT+2μ30,s-μ30,mRT=-lnc1sc1m-2lnc3sc3m

μ10,s-μ10,mRT+2μ30,s-μ30,mRT=lnc1sc1m-1c3sc3m-2

expμ10,s-μ10,mRT+2μ30,s-μ30,mRT=c1mc1sc3mc3s2

expμ10,s-μ10,mRTexpμ30,s-μ30,mRT2=c1mc1sc3mc3s2

δ10δ302=c1mc1sc3mc3s2

c1sc3s2δ10δ302=c1mc3m2

Maintaining electroneutrality such that,

z1c1s+z3c3s=0

z1c1m+z3c3m-|χ|=0

We can plug in the c1s and c1m terms,

c3s2c3s2δ10δ302=c3m+|χ|2c3m2

12c3s3δ10δ302=12c3m3+|χ|c3m2

c3s3δ10δ302=c3m3+|χ|c3m2

We set δ10δ30=δ* and obtain the co-ion form.

c3m3+χc3m2-c3s3δ*δ30=0

Taking this one step further where we define Hi=cimcis, divide each term by c3s3,

H33-χc3sH32-δ*δ30=0

Similarly, for LaCl3,

c1sc3s3δ10δ303=c1mc3m3

c3m4+χc3m3-c3s4δ*δ302=0

H34-χc3sH33-δ*δ30=0

Compiling the final-form equation for each single salt pairing investigated,

NaCl:

c1sc3sδ10δ30=c1mc3m

c3m2-χc3m-c3s2δ*=0

H32-χc3sH3- δ*=0

CaCl2:

c1sc3s2δ10δ302=c1mc3m2

c3m3+χc3m2-c3s3δ*δ30=0

H33-χc3sH32-δ*δ30=0

LaCl3:

c1sc3s3δ10δ303=c1mc3m3

c3m4+χc3m3-c3s4δ*δ302=0

H34-χc3sH33-δ*δ30=0

There is clearly a pattern emerging from these equations as you increase the valency of the cation (which, in this case, is the counter-ion).

Assuming δ1=δ2=γ1s= γ1m=γ2s= γ2m=1…

We obtain (eqs 58 and 59 in SI),

c1m|z3|c3m|z1|=H1|z3|H3|z1|c1s|z3|c3s|z1|

c2m|z3|c3m|z2|=H2|z3|H3|z2|c2s|z3|c3s|z2|

Here, we want to develop a relationship for c2m in terms of c1m. To do so, we begin by simplifying the exponents of the second equation by raising it to the exponent of  |z1||z2|. We obtain

c2m|z1||z3||z2|c3m|z1|=H2|z1||z3||z2|H3|z1|c2s|z1||z3||z2|c3s|z1|

Next, take the ratio of the two equations,

c1m|z3|c3m|z1|=H1|z3|H3|z1|c1s|z3|c3s|z1|c2m|z1||z3||z2|c3m|z1|=H2|z1||z3||z2|H3|z1|c2s|z1||z3||z2|c3s|z1|

The c3m, c3s, and H3 terms cancel out. After solving for c2m we obtain,

c2m=H2c1mH1c1s|z2||z1|c2s=H2H1theoH1|z2||z1|c2s

Now, we take the first equation above and plug in the electroneutrality constraints (eq 4, 31)

c1m|z3|c3m|z1|=H1|z3|H3|z1|c1s|z3|c3s|z1|

c1m|z3|z1c1m+z2c2m-|χ||z3||z1|=H1|z3|H3|z1|c1s|z3|z1c1s+z2c2s|z3||z1|

We define c2s=βc1s and substitute this along with the c2m relationship above, yielding

c1m|z3|z1c1m+z2H2c1mH1c1s|z2||z1|βc1s-|χ||z3||z1|=H1|z3|H3|z1|c1s|z3|z1c1s+z2βc1s|z3||z1|

After simplifying, we obtain

0=|z1||z1|c1m|z1|+|z3|+|z2|H2βc1sz11H1c1s|z2|c1mz2+z3-χz1c1mz3-H1|z3|H3|z1|c1s|z1|(|z1|+|z2|β)|z1|

Isolating for c1m yields

0=c1mz2+z3+|z1||z2|H2βc1sz1H1c1sz2c1mz1+z3-χz2H2βc1sz1H1c1sz2c1mz3-H1z2+z3c1sz1+z2H3z2H2βc1s(|z1|+|z2|β)z1

Since we are interested in H1theo=c1mc1s, we divide each term by c1sz2+z3,

0=c1mc1sz2+z3+|z1|z2H2βz1H1z2c1mc1sz1+z3-χz2H2βz1H1z2c1s-z1c1mc1sz3-H1z2+z3c1s-z3H3z2H2βc1s(|z1|+|z2|β)z1

We are interested in how the partition coefficient changes as a function of ionic strength. In this way, we can express the ion solution concentrations in terms of ionic strength. The definition of ionic strength is

Ionic strength I=12zi2c1s

I=12[z12c1s+z22c2s+z32c3s]

Rearranging to solve for c1sf(I),

c1s=2Iz1z1+z3+z2β(z2+z3)